QSCP Hamilton Inspection Department

Site: Hamilton Plant

NCR

| No. | Status | Date |
| --- | --- | --- |
| QSCP-NCR-2024-031 | Issued | 2024-11-05 |

# Nonconformance - 4-RA-101-06 Below t-min

## Scope and Responsibilities

This document addresses a critical wall loss condition identified during the 2024 thickness survey of the ATU-100. The scope is limited to the rich amine piping circuit 4-RA-101, specifically the localized thinning at 4-RA-101-06. Jennifer Walsh, acting as the Inspection Coordinator and API 570 inspector, is responsible for the technical validation of the ultrasonic data and the issuance of this nonconformance report.

The field data acquisition was performed by Larkhall NDE Services Inc. under the requirements of QSCP-IP-ATU100 Rev 3. Jennifer Walsh has reviewed the findings against the site retirement thickness criteria to determine the necessary mitigation and repair strategies for the Hamilton Plant asset integrity program.

## Inspection Findings and Data Analysis

During the execution of LNDE-FN-20241025-031, a thickness reading of 3.59 mm was recorded at 4-RA-101-06 on 2024-11-04. This value is below the established t-min of 3.81 mm for the 114.3 mm OD A106 Gr.B piping. The current reading indicates a significant acceleration in the corrosion rate compared to historical data recorded in 2014, 2016, and 2019.

The short-term corrosion rate has increased to 0.664 mm/y, resulting in an expired remaining life. This exceeds the 0.253 mm/y rate observed during the 2019 survey. Per the site rules for rich amine service, which is subject to a 3-year RBI interval under QSCP-IP-ATU100 Rev 3, the current wall thickness fails to meet the minimum structural requirements for the design limits of 862 kPa(g) and 82 °C.

## Nonconformance Description

The nonconformance is characterized by localized thinning at 4-RA-101-06 that has breached the retirement limit. While the nominal thickness of 4-RA-101 is 8.56 mm, the measured 3.59 mm represents a total loss of 4.97 mm. This condition was identified during the 150 CML survey documented in LNDE-FN-20241025-031.

The accelerated metal loss in this rich amine circuit indicates that the previous inspection interval was insufficient to capture the change in degradation morphology. The current state of 4-RA-101-06 violates the safety factors required for continued operation of the ATU-100 piping systems.

## Required Actions

Immediate engineering evaluation is required to determine if a temporary repair or a full component replacement is necessary before the next operational cycle. Jennifer Walsh will oversee the verification of the repair plan to ensure compliance with the site rules regarding t-min and remaining life calculations.

The inspection frequency for 4-RA-101 must be reassessed in QSCP-IP-ATU100 Rev 3 to account for the 0.664 mm/y corrosion rate. All future surveys must prioritize this circuit to prevent further excursions below the 3.81 mm retirement threshold.

| Sign-off | Name | Function | Date | Signature |
| --- | --- | --- | --- | --- |
| Prepared | Jennifer Walsh | Inspection Coordinator, API 570 inspector | 2024-11-05 | ______________ |