QSCP Corporate Asset Integrity

Corporate Summary

| No. | Status | Date |
| --- | --- | --- |
| QSCP-TRL-2013-01 | Issued | 21.05.2013 |

# Translation - ZÜS Periodic Inspection Report ANG-DA-2013-04120

## Executive Summary

This document provides the English translation of ANG-DA-2013-04120, issued by Anlagenüberwachung Niers GmbH on 2013-03-28. This was the first periodic ZÜS inspection performed by this body for ANLAGE-21. The inspection identified specific deficiencies regarding the integrity of the insulation systems on two stainless steel lines.

Daniel Hartmann has prepared this summary for QSCP Corporate Asset Integrity to ensure the findings are integrated into the corporate asset registry.

## Technical Findings and Line Data

The inspection focused on NR-21-L-0412 (K-2101 bottoms to E-2104, 88.9 mm x 3.2 mm) and NR-21-L-0415 (Reboiler circuit K-2101/E-2103, 168.3 mm x 4.0 mm). Both lines are constructed from 1.4404 and have design limits of PS 10 bar(g) and TS 150 °C. Minimum wall thicknesses per Werksnorm are 2.0 mm and 2.5 mm respectively.

ANG-DA-2013-04120 reports damaged cladding and wet insulation on both NR-21-L-0412 and NR-21-L-0415. Due to the presence of hot aqueous chlorides, these conditions present a risk to the 1.4404 material.

## Required Actions

The ZÜS report requires the removal of insulation at the affected locations to facilitate a Festigkeitsprüfung. Furthermore, surface crack testing (PT) must be carried out to identify any surface indications resulting from the moisture ingress. These actions are mandatory to maintain the integrity status of ANLAGE-21.

| Sign-off | Name | Function | Date | Signature |
| --- | --- | --- | --- | --- |
| Prepared | Daniel Hartmann | Integrity Engineer, QSCP Corporate Asset Integrity, based at Werk Niederrhein | 21.05.2013 | ______________ |